## Slide 1: force Shear
Shear Stress:
The stresses acting perpendicular to the surfaces considered are normal stresses and were discussed in the preceding section.
Now consider a bolted connection in which two plates are connected by a bolt with cross section A as shown in figure 1.
figure 1

## Slide 2: force Shear
The tensile loads applied on the plates will tend to shear the bolt at the section AA. Hence, it can be easily concluded from the free body diagram of the bolt that the internal resistance force V must act in the plane of the section AA and it should be equal to the external load P.
These internal forces are called shear forces and when they are divided by the corresponding section area, we obtain the shear stress on that section.
……… (1)
Equation 1 defines the average value of the shear stress on the cross section and the
distribution of them over the area is not uniform.
In general, the shear stress is found to be maximum at the centre and zero at certain
locations on the edge. This will be dealt in detail in shear stresses in beams .
In figure 1, the bolt experiences shear stresses on a single plane in its body and hence it
is said to be under single shear.

## Slide 3: force Shear
figure 2
In figure 2, the bolt experiences shear on two sections AA and BB. Hence, the bolt is said to be under double shear and the shear stress on each section is
…………(2)
Assuming that the same bolt is used in the assembly as shown in figure 1 and 2 and
the same load P is applied on the plates, we can conclude that the shear stress is reduced
by half in double shear when compared to a single shear.
Shear stresses are generally found in bolts, pins and rivets that are used to connect
various structural members and machine components.

## Slide 4: the Fracture and toughness in materials
if a material contains a crack, and is sufficiently stressed, the crack becomes unstable and grows at up to the speed of sound
in the material to cause catastrophically rapid fracture, or fast fracture at a stress less than the yield stress.
Mechanisms of crack propagation
1- ductile tearing
what happens when we load a cracked piece of ductile metal in other words, a metal that can flow readily to give large plastic deformations (like pure copper; or mild steel at, or above, room temperature).

## Slide 5: the Fracture and toughness in materials
If we load the material sufficiently, we can get fracture to take place starting from the crack. you see that the fracture surface is extremely rough, indicating that a great deal of plastic work has taken place. Let us explain this observation. Whenever a crack is present in a material, the stress close to the crack, local, is greater than the average stress applied to the piece of material; the crack has the effect of concentrating the stress.
The closer one approaches to the tip of the crack, the higher the local stress becomes until at some distance from the tip of the crack the stress reaches the yield stress, of the material, and plastic flow occurs .

## Slide 6: the Fracture and toughness in materials
Note that the zone of plasticity shrinks rapidly as yield stress increases: cracks in soft metals have a large plastic zone; cracks in hard ceramics have a small zone or none at all. Even when nominally pure, most metals contain tiny inclusions (or particles) of chemical compounds formed by the reaction between the metal and impurity atoms.
Within the plastic zone, plastic flow takes place around these inclusions, leading to elongated cavities, as shown in Figure 1. As plastic flow progresses, these cavities link up, and the crack advances by means of this ductile tearing. The plastic flow at the crack tip naturally turns our initially sharp crack into a blunt crack.

## Slide 7: the Fracture and toughness in materials
Figure 1
The important thing about crack growth by ductile tearing is that it consumes a lot of energy by plastic flow; the bigger the plastic zone, the more energy is absorbed. This is why ductile metals are so tough. Other materials, too, owe their toughness to this behavior plasticine is one, and some polymers also exhibit toughening by processes similar to ductile tearing.

## Slide 8: the Fracture and toughness in materials
2- cleavage
If you now examine the fracture surface of something like a ceramic, or glass, you see a very different state of affairs. Instead of a very rough surface, indicating massive local plastic deformation, you see a rather featureless, flat surface suggesting little or no plastic deformation. How is it that cracks in ceramics or glasses can spread without plastic flow taking place?
ceramics and glasses have very high yield strengths, and thus very little plastic deformation takes place at crack tips in these materials.
The energy required simply to break the interatomic bonds is much less than that absorbed by ductile tearing in a tough material, and this is why materials like ceramics and glasses are so brittle. It is also why some steels become brittle and fail like glass, at low temperatures.

## Slide 9: the Fracture and toughness in materials
At low temperatures metals having b.c.c. and c.p.h. structures become brittle and fail by cleavage, even though they may be tough at or above room temperature.
At lower temperatures, this thermal agitation is less, and the dislocations cannot move as easily as they can at room temperature in response to stress the intrinsic lattice resistance increases. The result is that the yield strength rises, and the plastic zone at the crack tip shrinks until it becomes so small that the fracture mechanism changes from ductile tearing to cleavage. This effect is called the ductile to brittle transition.