## Slide 1: Fatigue
Fatigue is a form of failure that occurs in structures subjected to dynamic and fluctuating stresses (e.g., bridges, aircraft, and machine components).
Under these circumstances, it is possible for failure to occur at a stress level considerably lower than the tensile or yield strength for a static load.
The term fatigue is used because this type of failure normally occurs after a lengthy period of repeated stress or strain cycling.
Fatigue is important inasmuch as it is the single largest cause of failure in metals, estimated to comprise approximately 90% of all metallic failures; polymers and ceramics (except for glasses) are also susceptible to this type of failure.

## Slide 2: fatigue
Furthermore, fatigue is catastrophic and insidious, occurring very suddenly and without warning.
Fatigue failure is brittle like in nature even in normally ductile metals, in that there is very little if any, gross plastic deformation associated with failure. The process occurs by the initiation and propagation of cracks, and ordinarily, the fracture surface is perpendicular to the direction of applied tensile stress.

## Slide 3: fatigue
the fatigue limit (also sometimes the endurance limit), below which fatigue failure will not occur. This fatigue limit represents the largest value of fluctuating stress that will not cause failure for essentially an infinite number of cycles. For many steels, fatigue limits range between 35% and 60% of the tensile strength.
fatigue strength, which is defined as the stress level at which failure will occur for some specified number of cycles.
fatigue life is the number of cycles to cause failure at a specified stress level.

## Slide 4: fatigue
CRACK INITIATION AND PROPAGATION
The process of fatigue failure is characterized by three distinct steps:
(1) crack initiation, wherein a small crack forms at some point of high-stress concentration.
(2) crack propagation, during which this crack advances incrementally with each stress cycle
(3) final failure, which occurs very rapidly once the advancing crack has reached a critical size.

## Slide 5: fatigue
FACTORS THAT AFFECT FATIGUE LIFE
1- Mean Stress
2- Surface Effects
3- Design Factors
4- Surface Treatments